## Slide 1: Saddle point search with dynamic active volume
Tao Liang, Haixuan Xu
The university of Tennessee Knoxville, Department of materials science and engineering
September 3rd 2025

## Slide 2: Installation
2
Follow the instructions to install anaconda.
Create a virtual environment.
  > conda create -p path_to_seakmc_env/seakmc_env
Activate the seakmc_env.
  >conda activate path_to_seakmc_env/seakmc_env
Install LAMMPS using conda.
  seakmc_env>conda install lammps=*=*mpich*
  or seakmc_env>conda install lammps=*=*openmpi*
Install OpenKIM package:
  seakmc_env>conda install openkim-models
Install pymatgen.
  seakmc_env>conda install --channel conda-forge pymatgen
Install mpi4py (version <=3.1.6).
  seakmc_env>python -m pip install mpi4py==3.1.6
Install SEAKMC_py_parallel.
seakmc_env>git clone https://github.com/TaoLiang120/SEAKMC_py_parallel.git
seakmc_env>cd SEAKMC_py_parallel
seakmc_env>python setup.py install or pip install .
SEAKMC_py itself does NOT include any energy or force evaluator. The python wrapper of LAMMPS (pyLAMMPS) is fully implemented in SEAKMC_py
It requires a dynamic LAMMPS library to install pyLAMMPS. If you have an external force field package that have an interface to LAMMPS, you need to compile it with a dynamic library.
conda create -p yourVenv python=3.12
conda activate yourVenv
conda install -c conda-forge pymatgen
conda install -c conda-forge cmake boost pybind11 fftw compilers libblas liblapack gfortran blas lapack
conda install -c conda-forge mpi4py=3.1.6
- add " -rdynamic" to "CPPFLAGS += -fPIC"
- add " -rdynamic" to "CXXFLAGS += -fPIC"
- add " -rdynamic -shared" to "FFLAGS += -fPIC"
Make file of the interface:
Install compilers in conda:
Follow the steps of LAMMPS /pyLAMMPS intallation:

## Slide 3: Outline
Background and introduction
  Dimer method
  Active volume
Dynamic active volume (DAV)
  Rescaling the dimer axis
Examples of SPS with DAV
  Fe-SIL
Implementation of SPS with DAV
  Flowchart
  Parallization scheme
  Determination of active volumes

## Slide 4: Dimer method
Translation steps
Energy (eV)
Elevation
Converging
0.64 eV
max
max
Elevation stage: dimer translates uphill
Converging stage: dimer translates downhill
G. Henkelman and H. Jonsson, JCP 111, (1999)
Dimer axis (N): a unit vector of R1 – R2
A2
A3
A4
A1
Notes: No detail on dimer method
Highlight elevation / converging stages
A SP that is immediately connecting between initial and final states are a connected sp

## Slide 5: Active volume
H. Xu and et al, J. Phy.: Condensed Matter 24, (2012)
H. Xu and et al, Comput. Mat. Sci. 100, (2015)
Saddle points are often involved in localized region
Active volume (AV) is constructed according to presence of defects
Seakmc (self-evolving atomistic kinetic Monte Carlo)
Notes: AV small enough to speed up sp
AV large enough that SP energy and positions are converged

## Slide 6: Existing challenges with saddle point search
H. Xu and et al., Comput. Mat. Sci. 100, (2015)
Max. potential energy increases with increasing size of AV
Probability of finding the saddle point decreases with increasing size of AV
vacancy
vacancy
Notes: 1) Max energy increases

## Slide 7: Dynamic active volume
Atom sequence (168 atoms)
Rescaling factors
RAS
LOGN
LOGN+RAS
Atomic disp. (
Atom sequence
RAS
LOGN
LOGN+RAS
Original
Dimer axis is a unit vector consisting of 3N components
RAS (Reverse atomic sequence): larger RAS means closer to the fixed atoms
LOGN defines as ln(), which is a value reflecting relative atomic displacements ()
DAV is applied only at elevation stage
Sigmoid rescaling
t
DAV: Applying rescaling factors on dimer axis at elevation stage
T. Liang and H. Xu, Comput. Mat. Sci. 228, (2023)
Deact.
Act.
Notes: Not much details

## Slide 8: Benchmark with point defects
8
Translation steps
Energy (eV)
Translation steps
Energy (eV)
Fe-vacancy (168 atoms)
Fe-dumbbell (610 atoms)
Notes: 1) # of atoms in AV

## Slide 9: Fe – Self interstitial loop (SIL)
9
[010]
[001]
∙
[100]
37-SIA cluster
37 self interstitial atom (SIA) cluster
Active volume of Fe-SIL[100] (2006 atoms)
System/active volume configuration:
Notes: An example of a complex defect, which requires a larger size of AV

## Slide 10: Fe – SILs with MCM2011 potential
10
Original
LOGN+RAS
Barrier (eV)
Displacement (Å)
Displacement (Å)
# of steps
200
500
1000
2000
2500
L. Proville and et al, Nature Materials 11, (2012)
9 SPs w. 1658 steps
301 SPs w. 594 steps
A 2006-atom AV
5000 attempts
2874 distinct saddle points for “Original” AV method, in which only 9 are connected
2408 distinct saddle points for DAV, in which 301 are connected

## Slide 11: Summary
11
Number of atoms
Time-efficiency improvement
Ratio of steps -1
Fe-dumbbell
Fe-SIL
Fe-vacancy
Cu56Zr44 glass
Time-efficiency improvement:
2) The improvement scales with the number of atoms in AV
Dynamic active volume can be applied if atomic displacements has a long-tail distribution
The time efficiency of a saddle point search with DAV can be significantly improved (42% to 179%)
The probability of finding the relevant saddle points using DAV has significantly increased
Summaries:

## Slide 12: Flowchart of code implementation
System inputs
Charactering AV
Loading DB
Finding Defects
Recycling
SNC
Finding PG
SP Search
Validating SPs
Save to DB
Post-processing SPs
KMC (LEB)
System relaxation
Barrier Recalibration
AV relaxation
To next KMC step, starting from Finding Defects
MD/Relax

## Slide 13: Parallization
13
Terminology:
  ntask_tot: total number of tasks
  nproc_task: number of processors per task
  ntask_proc: number of tasks per processor
  master_slave: master-slave work
ntask_tot: 1
nproc_task: max
no master-slave
ntask_tot: number of atoms
ntask_proc:
Evenly distributed
no master-slave
ntask_tot: number of AVs or SPs
nproc_task: large
master-slave
ntask_tot: number of SP searches
nproc_task: small
master-slave

## Slide 14: Communicator Split
14
Example with master-slave:
  size_world: 12
  nproc_task: 3
1) M received READY,
M send START/idtask or EXIT/None
2) M received Done, update completed_tasks, undo_jobs,
M send START/idtask or EXIT/None
3) M received EXIT, update completed_tasks
Master
Slaves
key or rank_split
0
1
2
idle
color
1) S send READY
2) if S received START/idtask, do work and send DONE/idtask
3) if S received EXIT, break and send EXIT
Four Tags:
READY, START, DONE, EXIT
0
1
2
3
while completed_tasks < ntask_tot:
while Tag == EXIT:

## Slide 15: Finding defective atoms
15
Available methods: BL, CN, BLCN, WS and custom
Chart: 
| 1 | 2 | 3 | 4 | 4 | 6 | 6 | 8 | 12
BL | 1.95 | 2.24 | 2.35 | 2.47 | 2.49 | 2.61 | 2.62 | 2.75 | 2.84
EPB | -12.82 | -6.53 | -5.19 | -4.13 | -4.31 | -2.8 | -3.19 | -2.7 | -1.73
Bond Length (Å)
Energy per Bond (eV)
bcc
fcc
sc
tri
dia
sq
hex
dimer
trimer
CN
Equilibrium BL increases as CN increases
absolute number of EPB decreases as BL increases
1. Local CN of an atom
2. Estimate equilibrium BL
Find a group of defective atoms (CN, BL strain or both)
Point defect reduction

## Slide 16: Building AV
16
colored by degree of overlapping
Allow overlapping: AV is constructed on each defect
Not allow overlapping: AV is constructed as a union of AVs of a defect chain ( a super defect)

## Slide 17: Input.yaml in flowchart
Kinetic_MC
potential
force_evaluator
data
“input.yaml”
active_volume
active_volume
Dynamic_matrix
SNC
Recycling
defect_bank
saddle_point
saddle_point
Validating SPs
Post-processing SPs
Post-processing SPs

## Slide 18: Parameters in active_volume
Point defect reduction
Active volume characteration
bondlengths: the equilibrium bond length of each bond type
coordnums: the coordination number of each species
Style: style of finding defects
NPredef: number of pre-determined defects
FindDefects: a set of parameters to identify point defects
PDReduction: point defect reduction
DCut4PDR:
RecursiveRed:
DActive: radius of active volume
Overlapping:
RT_SetMolID, R4RT_SetMolID, FCT4RT_SetMolID: a set of parameters to define the region for characterizing AV
potential:
active_volume:
If an atom’s –Npredef <= molecular-id < 0, this atom will be considered a defect and won’t characterize the AV.
DCut4PDR
If an atom’s molecular-id < -NPredef, this atom will be considered a defect and won’t characterize the AV.
Automatically add “molecular-id” entry

## Slide 19: Parameters in Dimer method
max
Dimer axis (N): a unit vector of R1 – R2
A2
A3
A4
A1
spsearch:
NSearch: # of SPS attempts
DimerSep: Dimer separation ()
HandleVN: a set of parameters for DAV
LocalRelax: a set of parameters for relaxation
force_evaluator: a set of parameters for force_evaluator in SPS
Preloading: a set of parameters for recycling saddle points. It will be used for guided SPS
ShowIterationResults: show iterations of each of SPS attempt
Notes: No detail on dimer method
Highlight elevation / converging stages
A SP that is immediately connecting between initial and final states are a connected sp

## Slide 20: Visual and output
Sel_iSPs: all
Write_Data_AV_SPs: True
Write_AV_SPs:
Write_Data_SPs:
Temporary folders:
Runner_i: a set of folders for ith job. The maximum number is the maximum jobs can be run simultaneously
Root directory:
  Seakmc.log
  Seakmc_summary.csv
SPOut directory:
  KMC_istep_Deleted.csv
  KMC_istep_SPs.csv
  KMC_istep_Prob.csv
  KMC_istep_DetailSPs.csv
DataOut directory:
  KMC_istep.dat
  KMC_istep_data_AVs.dat
  KMC_istep_Data_SP_isp.dat
  KMC_istep_Data_FI_isp.dat
AVOut directory:
  KMC_istep.dat
  KMC_istep_data_AVs.dat
  KMC_istep_Data_SP_isp.dat
  KMC_istep_Data_FI_isp.dat

## Slide 21
21
https://github.com/TaoLiang120/SEAKMC2_py_parallel
Code is coupled with Python LAMMPS
Code also has interfaces to VASP and LAMMPS binaries
Code download:
Interfaces with energy and force evaluators:
My email: tliang7@utk.edu